1. The density of potassium, which has the BCC structure and one atom per lattice point, is 0.855 g/cm3. The atomic weight of potassium is 39.09 g/mol. (10%) 
Calculate (a) the lattice parameter

(b) the atomic radius of potassium

2. A sample of BCC metal was placed in an X-ray diffractometer using X-rays with a wavelength of ( = 0.1541 nm. Diffraction from the {221} planes was obtained at 2( = 88.838°. Calculate a value for the lattice constant a for this BCC elemental metal. (Assume first-order diffraction, n = 1.) (10%)

3. Describe and illustrate the following planar defects: (a) twins, (b) low-angle tilt boundaries, (c) stacking faults. For each defect, express the impact on the properties of the material. (12%)

4. The following data were collected from a 20 mm diameter test specimen of a ductile cast iron (lo = 40.00 mm): (24%)

After fracture, the total length is 47.42 mm and the diameter is 18.35 mm. 
Calculate (a) the tensile strength, (b) the modulus of elasticity, (c) the % elongation,

(d) the % reduction in area, (e) the engineering stress at fracture,

(f) the true stress at fracture.

5. What are five important factors that affect the recrystallization process in metals? (10%)

6. Derive the lever rule for the amount in weight percent of each phase in two-phase regions of a binary phase diagram. Use a phase diagram in which two elements are completely soluble in each other. (10%)

7. The diffusion coefficient for Cr+3 in Cr2O3 is 6 × 10−15 cm2/s at 727oC and is 1 × 10−9 cm2/s at 1400oC. Calculate (a) the activation energy and

(b) the constant D0. R=8.314 J/mol(K(12%)

8. Consider a magnesium-iron galvanic cell consisting of a magnesium electrode in a solution of 1 M MgSO4 and an iron electrode in a solution of 1 M FeSO4. Each electrode and its electrolyte are separated by a porous wall, and the whole cell is at 25°C. Both electrodes are connected with a copper wire. (12%)

(a) Which electrode is the anode?

(b) Which electrode corrodes?

(c) What is the emf of the cell?

Table 1 Standard electrode potentials for selected elements at 25 oC

| Oxidation (corrosion) reaction | Electrode potential E0 (volts versus standard hydrogen electrode) |
| --- | --- |
| Li ( Li+ + e- | -3.05 |
| Mg ( Mg2+ + 2e- | -2.37 |
| Fe ( Fe2+ + 2e- | -0.44 |
| H2 ( 2H+ + 2e- | 0.00 |
| Cu ( Cu2+ + 2e- | +0.34 |

# Text boxes

綠色能源科技學系

碩士班

國立臺南大學 101學年度                      招生考試  材料科學  試題卷